**Constructing AgI/BiSI p-n heterojunctions with an internal electric field for efficient degradation of refractory organic pollutants**

Jin Liua,\*, Qian Zhonga, Yanjin Wanga, Zezhi Zhanga, Huiqin Zhenga,\*, Bin Yanb, Yurong Shib

*a College of Environmental Economics, Henan Finance University, Zhengzhou 450046, China*

*b School of Materials Science and Engineering, North China University of Water Resources and Electric Power, Zhengzhou, 450000, China*

\*Corresponding author. E-mail addresses: liuzejin1026@126.com (J. Liu); zhenghuiqin2000@163.com (H.Q. Zheng)



**Fig. S1.** Degradation rate and TOC rate of AR1 over 3AgI/BiSI under visible light irradiation.



**Fig. S2.** Effects of (a) AR1 concentration and (b) pH values on the photocatalytic performances of 3AgI/BiSI.

**Table S1.** The electrical properties of AgI and BiSI obtained by Hall effect measurements.

|  |  |  |  |  |
| --- | --- | --- | --- | --- |
| Samples | Carrier concentration(cm-3) | Resistivity(Ω·cm) | Hall mobility(cm2 V-1 s-1) | Conduction type |
| AgI | 1.864×1013 | 2.272×103 | 1.452×102 | p |
| BiSI | 3.023×1012 | 1.053×105 | 9.826 | n |

**Table S2.** Comparison of AR1 degradation over different reported different photocatalysts.

|  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| Catalyst type | Catalyst dose (g) | AR1 concentration (mg L-1) | AR1volume (mL) | Light source | k(min-1) | Ref. |
| TiO2/glass microspheres | 0.03 | 40 | 50 | 20 W UV lamp | 0.0103 | [1] |
| ZnAl2O4/CuS | 0.2 | 20 | 200 | 4×17 W UV lamp | 0.030 | [2] |
| AgI/Bi2Ga4O9 | 0.02 | 20 | 50 | 100 WLED lamp (λ=420 nm) | 0.2539 | [3] |
| Ag-Li-ZnO | 0.05 | 5 | 50 | 300 W tungsten lamp | 0.0181 | [4] |
| AgI/BiSI | 0.05 | 30 | 100 | 100 W LED lamp (λ=420 nm) | 0.4699 | This work |

**References**

[1] Y. Zhang, M. Han, Y.J. Tao, W.J. Zhang, H. Wang, Sol-gel synthesis of suspensible titanium dioxide-hollow glass microsphere composites for photocatalytic degradation of Acid Red 1, Ceram. Int., 46 (2020) 22846-22853, https://doi.org/10.1016/j.ceramint.2020.06.053.

[2] Y. Fahoul, M. Zouheir, K. Tanji, A. Kherbeche, Synthesis of a novel ZnAl2O4/CuS nanocomposite and its characterization for photocatalytic degradation of acid red 1 under UV illumination, J. Alloys Compd., 889 (2021) 161708, https://doi.org/10.1016/j.jallcom.2021.161708.

[3] Y. Liu, H. Zou, H. Ma, J. Ko, W. Sun, K. Andrew Lin, S. Zhan, H. Wang, Highly efficient activation of peroxymonosulfate by MOF-derived CoP/CoOx heterostructured nanoparticles for the degradation of tetracycline, Chem. Eng. J., 430 (2022) 132816, 10.1016/j.cej.2021.132816.

[4] K. Masula, R. Kore, Y. Bhongiri, S. Pola, M. Basude, Ag-Li-ZnO nanostructures for efficient photocatalytic degradation of organic dyes and textile wastewater under visible light treatment, J. Mol. Struct., 1305 (2024) 137750, https://doi.org/10.1016/j.molstruc.2024.137750.