Cellulose Nanocrystals Isolated from Sugarcane Bagasse Using the Formic/ Peroxyformic Acid Process: Structural, Chemical, and Thermal Properties

An Nang Vu  a, b, *, Long Hoang Nguyen  a, b, Kimio Yoshimura d, Tap Duy Tran a, b, Hieu Van Le  a, b, c

a Faculty of Materials Science and Technology, University of Science, VNU–HCM, 700000, Vietnam.

b Vietnam National University Ho Chi Minh City, 700000, Vietnam.

c Laboratory of Multifunctional Materials, University of Science, VNU–HCM, 700000, Vietnam.

d Department of Advanced Functional Materials Research, Takasaki Advanced Radiation Research Institute, National Institutes for Quantum Science and Technology (QST), Takasaki, Gunma 370-1292, Japan

* Corresponding author. E-mail address: vnan@hcmus.edu.vn

Supporting Information

Fig. S1. Each XRD peak of treated SCB was deconvoluted by crystalline and amorphous peaks, and the CrI chart

Table S1. Thermal properties of SCB at different stages of treatment

| Sample | Tonset (⁰C) | Tmax (⁰C) | Wloss (%) | Tonset (⁰C) | Tmax (⁰C) | Wloss (%) | Tonset (⁰C) | Tmax (⁰C) | Wloss (%) | Char Yield at 800 ⁰C (%) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Water evaporation |  |  | 1st. Thermal degradation |  |  | 2nd. Thermal degradation |  |  |  |
| Raw | 39.0 | 60.8 | 6.5 | 221.9 | 242.4 | 12.4 | 323.4 | 386.7 | 73.1 | 8.0 |
| Acid-treated | 39.0 | 79.1 | 7.8 | - | - | - | 367.3 | 397.3 | 82.1 | 10.0 |
| PFA-treated | 29.0 | 74.5 | 7.7 | - | - | - | 360.8 | 390.5 | 82.8 | 9.5 |
| Bleached | 33.5 | 80.6 | 6.4 | - | - | - | 359.2 | 395.8 | 81.4 | 12.1 |
| CNCs | 28.0 | 66.2 | 7.1 | 239.4 | 250.0 | 35.2 | 362.9 | 410.2 | 32.3 | 25.4 |

Fig. S2. 13C NMR spectra of bleached SCB and CNCs