Supporting Information

Highly efficient crystalline-amorphous Fe2O3/Fe-OOH oxygen evolution electrocatalysts reconstructed by FeS2 nanoparticles

Xiaozhen Rena*, Shanshan Lia, Ziyou Lia, Zhenyang Zhanga, Hanxu Houa, Yanan Zhoua, Chuanyu Jina*

a: School of Materials Science and Engineering, Liaocheng University, Liaocheng, 252000, China

* Corresponding authors: 1 Hunan Road, Liaocheng City, Shandong Province, China

Fig. S1 XPS of Fe0.25Co0.75S2 samples

Fig. S2 Raman spectra of CoS2, Co0.25Fe0.75S2 and FeS2 (cm-1)

In order to better understand the intrinsic activity, the turnover frequency (TOF) of all the samples for OER at the same potential had been provided.

To calculate the per-site turnover frequency (TOF), we used the following formula1:

The total number of oxygen turn overs was calculated from the current density according to the following conversion:

Since the exact oxygen binding site is not known, we estimated the number of sites as the number of sample molecular calculated based on the mass of the samples used in the electrochemical measurements according to the following conversion:

Based on the current density at the same overpotential (300 mV), the per site TOF was determined as follows:

According to the above calculations, the TOF value of FeS2 for OER at the overpotential of 300 mV is higher, indicating the better catalytic activity.

Fig. S3 Cyclic voltammetry curve of various samples at scan rates of 20, 40, 60, 80, 100 mv/s in 1 M KOH.

Fig. S4 Raman spectra of survey for FeS2 before and after OER

Fig. S5 The water contact angle on FeS2