Supplementary Material (SM)

Near-infrared optical properties of Cs2KScF6:Cr3+ phosphor for high-power light-emitting diodes

Lingxiang Chu, Enbei Yang, Han Ma, Jing Wan*, Tao Yang, Yi Qin, Yanqing Ye, Qiang Zhou*, Zhengliang Wang

Key Laboratory of Green Chemistry Materials in University of Yunnan Province, Yunnan Key Laboratory of Chiral Functional Substance Research and Application, School of Chemistry and Environment, Yunnan Minzu University, Kunming 650500, P. R. China.

Corresponding Author:

*Email: jwan@ymu.edu.cn (J. Wan)

q-zhou@ymu.edu.cn (Q. Zhou)

The luminescence of Cr3+ ions is highly dependent on crystal field strength provided by matrix. Generally, Cr3+ ion emits broadband NIR light from 4T2 → 4A2 transition in a weak coordination field with Dq/B < 2.3, whereas produces sharp line or narrowband emission from 2E → 4A2 transition in a strong crystal field with Dq/B > 2.3. The parameters of Dq and B were calculated by the following equations [S1]:

10Dq=E4T2=E4A2→4T2                      (S1)

DqB= 15（∆E/Dq-8）（∆E/Dq)2-10(∆E/Dq)                            (S2)

where ΔE denotes the energy difference determined by the PLE peak values of 4A2 → 4T1 (435 nm) and 4A2 → 4T2 (657 nm) transitions. The Dq/B value is calculated as 1.74 in this case, revealing Cr3+ ions experience a weak crystal field in the Cs2KScF6 host.

All decay curves of Cs2KScF6:Cr3+ phosphor comply with a single-exponential equation [S2]:

It= I0+Aexp-tτ                              (S3)

where It represents the luminescence intensity, I0 denotes initial luminescence intensity. A and τ mean constant and the decay time, respectively.

In order to illustrate the concentration quenching mode of phosphor, the critical distance (Rc) between Cr3+ ions was estimated via the following formula established by Blass [S3,S4]:

RC≈2(3V4πxcN)1/3                                (S4)

where N is the substitution number in a unit cell, V represents the unit cell volume. In this case, N = 4, V = 776.96 Å, xc = 0.05, Rc is then calculated to be 19.51 Å, suggesting multipolar interaction is the main reason for non-radiative energy transfer in Cs2KScF6 host.

According to Dexter theory, the main type of multipolar interaction was evaluated using the following equation [S5]:

Ix = k1+β(x)θ/3-1                           (S5)

Here, I and x stand for integral emission intensity and activator concentration, respectively. k and β are constants under the same excitation condition. By fitting log(I/x) versus log(x), a linear relationship with a slope of -0.801 was obtained, indicating the θ value is equal to 2.403.

For evaluating the electron-phonon coupling strength of Cs2KScF6:Cr3+ phosphor, we calculated the Huang-Rhys factor (S) with the following formula [S6]:

FWHM2=5.57×S×(ћω)2×(1+2kTћω)                 (S6)

Here, ћω means the maximum phonon energy, k is the Boltzmann constant. Based on the temperature-dependent PL spectra, a linear relationship with reliable correlation coefficient of 0.987 is obtained by taking FWHM2 as a function of 2kT, indicating ћω and S are 0.043 eV and 1.68, respectively.

The thermal quenching activation energy (ΔE) of Cs2KScF6:Cr3+ phosphor could be calculated by the modified Arrhenius formula [S7]:

IT=I0/[1+Ae(-ΔE/kT)]                           (S7)

Here, I0 symbolizes the initial PL intensity, IT is luminescent intensity at temperature T, A represents a refined constant and k is the Boltzmann constant. By employing ln[(I0/IT)-1] as a function of 1/kT, ∆E is fitted to be 0.340 eV.

Fig. S1. XRD pattern of (NH4)3CrF6.

Fig. S2. SEM, EDS and elemental mapping results of Cs2KScF6:Cr3+ sample.

Fig. S3. Tanabe-Sugano diagram of Cr3+ in octahedral crystal field.

Fig. S4. PL spectra and relative PL intensity of Cs2KScF6:0.05Cr3+ phosphor aged for 132 h at a high temperature (85 ℃) and high humidity (85%) conditions.

Fig. S5 Normalized temperature-dependent PL spectra of Cs2KScF6:0.05Cr3+ phosphor.

Fig. S6 Thermographs of NIR pc-LED device operating at 200 mA for 10, 20, 30, 40, 50, 60 minutes.

Table S1. The crystallographic parameters of Cs2KScF6 host and Cs2KScF6:0.05Cr3+ sample.

| Formula | Cs2KScF6 | Cs2KScF6:0.05Cr3+ |
| --- | --- | --- |
| Crystal system | Cubic | Cubic |
| Space group | Fm33m(225) | Fm33m(225) |
| a (Å) | 9.33 | 9.19 |
| b (Å) | 9.33 | 9.19 |
| c (Å) | 9.33 | 9.19 |
| α | 90.0000 | 90.0000 |
| β | 90.0000 | 90.0000 |
| γ | 90.0000 | 90.0000 |
| V (Å3) | 812.21 | 776.96 |
| Z | 4 | 4 |
| Rwp (%) | - | 9.60% |
| Rp(%) | - | 8.91% |
| χ2 | - | 2.321 |

Table S2. Photoelectric properties of LED devices prepared by Cr3+-activated NIR phosphors.

| Phosphor | Wavelength (nm) | Dq/B | NIR output power (mW) | Conversion efficiency | Reference |
| --- | --- | --- | --- | --- | --- |
| LiMgGaF6:Cr3+ | 803 | 2.137 | 60.78@360 mA | 5.7%@360 mA | [S8] |
| LiMgAlF6:Cr3+ | 734 | 2.03 | 24.3@320 mA | 6.3%@20 mA | [S9] |
| LiScP2O7:Cr3+ | 880 | 1.84 | ~ 19@100 mA | ~ 12%@100 mA | [S10] |
| K3AlF6:Cr3+ | 763 | - | 5.5@150 mA | - | [S11] |
| Na3GaxAl1-xF6:Cr3+ | 756 | 2.04 | 78.45@400 mA | 6.53%@350 mA | [S12] |
| Na3Al2Li3F12:Cr3+ | 750 | 1.95 | 14.3@60 mA | - | [S13] |
| ScBO3:Cr3+ | 800 | 2.88 | 39.11@350 mA | - | [S14] |
| BaMgAl10O17:Cr3+ | 762 | 2.47 | 3.4@100 mA | - | [S15] |
| NaInGe2O6:Cr3+ | 900 | 1.89 | 25.2@120 mA | 4.8%@120 mA | [S16] |
| Cs2KScF6:Cr3+ | 778 | 1.74 | 72.28@320 mA | 6.83%@120 mA | This work |

Reference:

[S1] A. Trueba, J. M. García-Lastra, P. Garcia-Fernandez, J. A. Aramburu, M. T. Barriuso, M. Moreno, Cr3+-doped fluorides and oxides: role of internal fields and limitations of the Tanabe-Sugano approach, J. Phys. Chem. A. 115 (2011) 13399–13406.

[S2] Y. Yan, M. Shang, S. Huang, Y. Wang, Y. Sun, P. Dang, J. Lin, Photoluminescence properties of AScSi2O6:Cr3+ (A = Na and Li) phosphors with high efficiency and thermal stability for near-infrared phosphor-converted light-emitting diode light sources, ACS Appl. Mater. Interfaces. 14 (2022) 8179–8190.

[S3] Y. Zhou, X. Li, T. Seto, Y. Wang, A high efficiency trivalent chromium-doped near-infrared-emitting phosphor and its NIR spectroscopy application, ACS Sustainable Chem. Eng. 9 (2021) 3145–3156.

[S4] Z. Ye, Z. Wang, Q. Wu, X. Huo, H. Yang, Y. Wang, D. Wang, J. Zhao, H. Suo, P. Li, A single luminescence center ultra-broadband near-infrared LiScGeO4:Cr phosphor for biological tissue penetration, Dalton Trans. 50 (2021) 10092–10101.

[S5] D. Dai, Z. Wang, Z. Xing, X. Li, C. Liu, L. Zhang, Z. Yang, P. Li, Broad band emission near-infrared material Mg3Ga2GeO8:Cr3+: substitution of Ga-In, structural modification, luminescence property and application for high efficiency LED, J. Alloys Compd. 806 (2019) 926–938.

[S6] X. Zhou, W. Geng, J. Li, Y. Wang, J. Ding, Y. Wang, An ultraviolet-visible and near-infrared-responded broadband NIR phosphor and its NIR spectroscopy application, Adv. Opt. Mater. 8 (2020) 1902003.

[S7] C. Jin, R. Li, Y. Liu, L. Zhang, J. Zhang, P. Sun, Z. Luo, J. Jiang, Efficient and stable Gd3Ga5O12:Cr3+ phosphors for high-performance NIR LEDs, Adv. Opt. Mater. 11 (2023) 2300772.

[S8] W. D. Nie, J. X. Zuo, S. Yang, Y. Li, W. F. Zou, G. Chen, S. H. Wu, D. Wu, S. B. Liu, J. Q. Peng, L. Han, X. Y. Ye, Ultra-broad NIR emission from two-site Cr3+ occupation in fluoride phosphor via composition-driven structural transformation, Mater. Today Chem. 26 (2022) 101164.

[S9] X. Hu, X. Li, Q. Yang, Y. Ye, Z. Wang, Q. Zhou, H. Tang, Q. Wang, A highly thermo-stable far-red LiMgAlF6:Cr3+ phosphor for plant-growth lighting, J. Lumin. 263 (2023) 120095.

[S10] L. Yao, Q. Shao, S. Han, C. Liang, J. He, J. Jiang, Enhancing near-infrared photoluminescence intensity and spectral properties in Yb3+ codoped LiScP2O7:Cr3+, Chem. Mater. 32 (2020) 2430–2439.

[S11] Q. Song, Z. Liu, H. Jiang, Z. Luo, P. Sun, G. Liu, Y. Liu, H. Jiang, J. Jiang, The hydrothermally synthesis of K3AlF6:Cr3+ NIR phosphor and its performance optimization based on phase control, J Am Ceram Soc. 104 (2021) 5235–5243.

[S12] J. Zhou, P. Chen, J. Li, M. Yang, W. Jiang, Q. Zhang, H. Ni, J. Huo, Crystal-field induced tuning of luminescence properties of Na3GaxAl1−xF6:Cr3+ phosphors with good thermal stability for NIR LEDs, Dalton Trans. 51 (2022) 10965.

[S13] D. Huang, S. Liang, D. Chen, J. Hu, K. Xu, H. Zhu, An efficient garnet-structured Na3Al2Li3F12:Cr3+ phosphor with excellent photoluminescence thermal stability for near-infrared LEDs, Chem. Eng. J. 426 (2021) 131332.

[S14] M. H. Fang, P. Y. Huang, Z. Bao, N. Majewska, T. Leśniewski, S. Mahlik, M. Grinberg, G. Leniec, S.M. Kaczmarek, C.W. Yang, K.M. Lu, H.S. Sheu, R.S. Liu, Penetrating biological tissue using light-emitting diodes with a highly efficient near-infrared ScBO3:Cr3+ Phosphor, Chem. Mater. 32 (2020) 2166–2171.

[S15] L. You, R. Tian, T. Zhou, R. Xie, Broadband near-infrared phosphor BaMgAl10O17:Cr3+ realized by crystallographic site engineering, Chem. Eng. J. 417 (2021) 129224.

[S16] W. Zhou, J. Luo, J. Fan, H. Pan, S. Zeng, L. Zhou, Q. Pang, X. Zhang, Luminescent properties and LED application of broadband near-infrared emitting NaInGe2O6:Cr3+ phosphors, Ceram. Int. 47 (2021) 25343–25349.