Supplementary Material

Biochar/poly(aniline-pyrrole) modified graphite electrode and electrochemical behavior for application in low-cost supercapacitor

M. Mahabur Rahman,a Abdulla Al Mamun,a Hideto Minami,b M. Mahbubor Rahman,a S. Manjura Hoque,c Hasan Ahmada

a Research Laboratory of Polymer Colloids and Nanomaterials, Department of Chemistry, Rajshahi University, Rajshahi 6205, Bangladesh

b Graduate School of Engineering, Kobe University, Kobe 657-8501, Japan

c Materials Science Division, Bangladesh Atomic Energy Commission, Dhaka, Bangladesh

*Corresponding author.

Email: samarhass@yahoo.com; hahmad@ru.ac.bd

ORCID ID: 0000-0003-1499-167X

Fig. S1. Preparation scheme of BC/P(Ani-Py) composite particles in two steps.

Fig. S2. FT-IR spectra of (a) BC seed particles, (b) P(Ani-Py) particles, (c) BC/P(Ani-Py)1:0.7 and (d) BC/P(Ani-Py)1:1 composite particles recorded in KBr pellets.

Fig. S3. TEM images of (a) BC seed particles, (b) P(Ani-Py) particles, (c) BC/P(Ani-Py)1:0.7 and (d) BC/P(Ani-Py)1:1 composite particles.

Fig. S4. XRD patterns of (a) BC seed particles, (b) P(Ani-Py) particles, (c) BC/P(Ani-Py)1:0.7 and (d) BC/P(Ani-Py)1:1 composite particles.

Table S1. Recipe for BC/P(Ani-Py) composite preparation.a)

|  | BC to mixed monomers (w/w) ratio |  |
| --- | --- | --- |
| Ingredients | 1:0.7 | 1:1 |
| BC (g) | 1.0175 | 1.0342 |
| Aniline (g) | 0.3549 | 0.5612 |
| Pyrrole (g) | 0.3586 | 0.5294 |
| APS (g) | 1.4637 | 2.1265 |
| Triton X-405 (g) | 0.2069 | 0.2153 |
| 0.1 M HCl (mL) | 50 | 50 |
| DD water (mL) | 50 | 50 |

a) 25 °C, 500 rpm, N2 gas, 24 h

Abbreviation: BC, biochar; APS, ammonium persulfate

Table S2. Parameters for EIS data fitting of C/P(Ani-Py)1:1 modified electrode.

| Elements | Value (Ω) |
| --- | --- |
| R1 | 4.037 |
| R2 | 0.0124 |
| W0 | 0.472 |
| CPE | 1.000 |

Table S3. Comparison of Energy density and Power density of various carbon rich electrode-based super capacitors.

| Electrode Materials | Energy density (Wh/kg) | Power density (W/kg) | Reference |
| --- | --- | --- | --- |
| Nitrogen doped micro-mesoporous carbon | 9.14 | 500 | Okonkwo et al., 2020 |
| CNTs/graphene/polyhedron | 68.6 | 800 | Liu et al., 2022 |
| CNTs/graphene/activated carbon | 6.6 | 69 | Rustamaji et al., 2022 |
| Phytic acid-doped poly(aniline-co-pyrrole) | 12.2 | 500 | Wang et al., 2020 |
| Chitosan-derived hybrid porous carbon | 34 | 900 | Yuan et al., 2019 |
| Self-graphenized bicohar | 25.56 | 500 | Xue et al., 2023 |
| BC/P(Ani-Py)1:1 modified graphite electrodes | 31.5 | 400 | This work |

References

Liu, Y., Ma, Z., Chen, X., Ying, Y., Shi, W., 2022. In-situ generated NiCo2O4/CoP polyhedron with rich oxygen vacancies interpenetrating by P-doped carbon nanotubes for high performance supercapacitors. J. Colloid Interface Sci. 608, 2246–2256. https://doi.org/10.1016/j.jcis.2021.10.099.

Okonkwo, C.A., Lv, T., Hong, W., Li, G., Huang, J., Deng, J., Guo, M., 2020. The synthesis of micromesoporous carbon derived from nitrogen-rich spirulina extract impregnated castor shell based on biomass self-doping for highly efficient supercapacitor electrodes. J. Alloys Compds. 825, 154009. https://doi.org/10.1016/j.jallcom.2020.154009.

Rustamaji, H., Prakoso, T., Devianto, H., Widiatmoko, P., Nurdin, I., 2022. Design, Fabrication, and testing of supercapacitor based on nanocarbon composite material. ASEAN J. Chem. Eng. 22 (1), 19–32. https://doi.org/10.22146/ajche.70139.

Wang, Y., Ma, WB., Guo, L., Song, X.-Z., Tao, X.-Y., Guo, L.-T., Fan, H.-L., Zhu, Y.-B., Wei, X.-Y., 2020. Phytic acid-doped poly(aniline-co-pyrrole) copolymers for supercapacitor electrodes applications. J Mater Sci: Mater Electron. 31, 6263–6273. https://doi.org/10.1007/s10854-020-03181-5.

Xue, C., Li, X., Du, J., Wang, L., Li, X., Yan, W., Hao, X., 2023. Self-graphenized biochar with huge pore volume prepared from pre-boiled Ulva lactuca for electrochemical supercapacitor with high energy density. J. Ener. Storage 72, 108498. https://doi.org/10.1016/j.est.2023.108498.

Yuan, M., Zhang, Y., Niu, B., Jian, F., Yang, X., Li, M., 2019. Chitosan-derived hybrid porous carbon with the novel tangerine pith-like surface as supercapacitor electrode. J. Mater. Sci. 54 (23), 14456–14468. https://doi.org/10.1007/s10853-019-03911-z.