Supplementary Material

# Mineralogical and geochemical characteristics of barium slag and ecological risks associated with heavy metals

Chengbing Fu a, b, c, Yu Zhang b, c, Juan Tian d, Wenxing Chen d, Hongyan Pan b, c, Jianxin Cao a, b, c, *

a College of Resources and Environmental Engineering, Guizhou University, Guiyang, Guizhou 550025, China

b School of Chemistry and Chemical Engineering, Guizhou University, Guiyang, Guizhou 550025, China

c Guizhou Key Laboratory for Green Chemical and Clean Energy Technology, Guizhou University, Guiyang, Guizhou 550025, China

d Guizhou Chemical Research Institute, Guiyang, Guizhou 550003, China

* Corresponding Author:

E-mail: jxcao@gzu.edu.cn

Table S1. Statistics of BS screening results.

| Number | wt (%) |
| --- | --- |
| BS1 | 52.55 |
| BS2 | 13.52 |
| BS3 | 13.10 |
| BS4 | 9.330 |
| BS5 | 11.50 |
| Total | 100.0 |

Table S2. Chemical composition distribution (wt%) in BS with different particle size.

| Chemical compositions | ≥850 μm (BS1) | 425-850 μm (BS2) | 150-425 μm (BS3) | 75-150 μm (BS4) | ＜75 μm (BS5) | Total |
| --- | --- | --- | --- | --- | --- | --- |
| SiO2 BaO SO3 CaO Al2O3 Fe2O3 MgO Na2O K2O TiO2 P2O5 SrO V2O5 ZnO MnO | 50.84 48.69 45.75 54.93 52.77 50.74 52.08 40.97 56.16 51.36 61.63 51.30 56.29 50.41 51.07 | 14.62 12.73 12.29 13.69 14.30 11.02 13.28 14.74 14.70 14.25 13.84 12.72 14.11 10.68 14.55 | 13.34 12.90 12.75 11.65 15.04 11.20 13.93 17.45 12.55 15.43 11.05 12.79 9.120 12.00 13.19 | 7.020 11.09 12.87 7.730 9.140 9.490 10.42 12.21 7.340 8.990 5.680 9.500 7.260 10.27 8.420 | 6.620 14.60 16.36 12.00 8.750 17.54 10.29 14.63 9.250 9.980 7.800 13.69 13.22 16.64 12.77 | 100.0 100.0 100.0 100.0 100.0 100.0 100.0 100.0 100.0 100.0 100.0 100.0 100.0 100.0 100.0 |

Table S3. Heavy metal distribution (%) in BS with different particle size.

| Heavy metal | ≥850 μm (BS1) | 425-850 μm (BS2) | 150-425 μm (BS3) | 75-150 μm (BS4) | ＜75 μm (BS5) | Total |
| --- | --- | --- | --- | --- | --- | --- |
| Cu Zn Pb Cr Cd Ni Fe Mn As Ba | 50.44 49.85 59.68 51.52 52.08 56.64 51.04 52.24 51.61 45.39 | 10.97 11.71 14.06 12.11 12.15 13.10 10.99 12.98 11.25 11.48 | 11.39 12.55 8.270 12.16 11.77 13.67 11.07 12.31 10.62 15.44 | 10.15 10.20 6.830 9.010 9.520 11.17 9.650 9.110 9.840 12.30 | 17.05 15.69 11.16 15.20 14.49 5.430 17.25 13.35 16.69 15.40 | 100.0 100.0 100.0 100.0 100.0 100.0 100.0 100.0 100.0 100.0 |

Fig.S1. Representative elemental mappings (C, O, Al, Si, S, Ca, Cr, Mn, Fe, Ni, Cu, Zn, As, Cd, Ba and Pb) of the BS1.

Fig.S2. Representative elemental mappings (C, O, Al, Si, S, Ca, Cr, Mn, Fe, Ni, Cu, Zn, As, Cd, Ba and Pb) of the BS2.

Fig.S3. Representative elemental mappings (C, O, Al, Si, S, Ca, Cr, Mn, Fe, Ni, Cu, Zn, As, Cd, Ba and Pb) of the BS3.

Fig.S4. Representative elemental mappings (C, O, Al, Si, S, Ca, Cr, Mn, Fe, Ni, Cu, Zn, As, Cd, Ba and Pb) of the BS4.

Fig.S5. Representative elemental mappings (C, O, Al, Si, S, Ca, Cr, Mn, Fe, Ni, Cu, Zn, As, Cd, Ba and Pb) of the BS5.